Specification clauses

To be read with Preliminaries/General conditions

Open mesh steel panel decorative fencing/gates

CLD ScreenFence 358 Rigid Mesh Panel System.

• Height:	1830mm/2030mm/2440mm/3000mm (other heights are available on request) * delete as required

• Nominal height: 	1.8m/2.0m/2.4m/3.0m (other heights are available on request) * delete as required

• Mesh & wire: 	76.2 x 12.5 mm mesh; 4 mm wire, high aluminium content galvanised and polyester powder-coated to minimum 80 microns

• ScreenFence Weave: 	Full Panel Weave Vertical

• Posts: 	80 x 60 mm special flanged section, hot-dipped galvanised after manufacture and polyester powder-coated to match fencing.

• Corner Posts: 	80 x 80 mm SHS, galvanised after manufacture and polyester powder-coated to match fencing.

• Fixings: 		M8 cup square bolt with permacone nut, galvanised.

• Set posts: 	Set posts in holes 450 mm diameter x 1000** mm deep, filled not less than half the depth with concrete, as clause 620.

• Maximum post centers: 	2520mm

• Other requirements: 	A full range of RAL Colours are available including marine grade and metallics.

A full range of ScreenFence Weaves are available.

** Depending on fence height and ground conditions

NOTES: 	All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.