Specification clauses

To be read with Preliminaries/General conditions

Open mesh steel panel perimeter security fencing/gates

CLD Securus Lite 358 Rigid Mesh Panel System.

• Height:	1200mm/1800mm/2000mm/2100mm/2400mm/3000mm (Heights up to 5200mm are available please contact CLD Fencing Systems for more information on post specifications) * delete as required

• Nominal height: 	1.2m/1.8m/2.0m/2.1m/2.4m/3.0m (Heights up to 5.2m are available) * delete as required

• Mesh & wire: 	76.2 x 12.5 mm mesh; 4 mm wire, high aluminium content galvanised and polyester powder-coated to minimum 80 microns

• Posts: 	60 x 60 mm SHS, galvanised after manufacture and polyester powder-coated with 30 x 5mm full length clamp bar galvanised and polyester powder-coated to match fencing. (1200mm – 2400mm Panels ONLY) * delete as required

80 x 40 mm RHS, galvanised after manufacture and polyester powder-coated with 30 x 5mm full length clamp bar galvanised and polyester powder-coated to match fencing. (3000mm Panels ONLY) * delete as required

• Fixings: 		M8 cup square bolt with permacone nut, galvanised.

• Set posts: 	Set posts in holes 300 mm diameter x 800** mm deep, filled not less than half the depth with concrete, as clause 620.

• Maximum post centers: 	2440mm

• Bottom of fencing to be: 	approx. 50 mm above final ground level. * delete as required

300mm Ground Bury. * delete as required

• Other requirements: 	PPC Colour Green RAL 6005. A full range of RAL Colours are available including marine grade and metallics.

** Depending on fence height

NOTES: 	All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.