Specification clauses

To be read with Preliminaries/General conditions

Open steel panel louvre perimeter security fencing/gates

CLD Screenogril Louvred Rigid Panel System.

• Height:	80/20 vision 954mm/1183mm/1596mm/1963mm (fencing can be made up of a combination of the above panels) * delete as required

100/0 vision 967mm/1196mm/1608mm/1975mm (fencing can be made up of a combination of the above panels) * delete as required

• Nominal height: 	1.0m/1.2m/1.6m/2.0m (fencing can be made up of a combination of the above panels) * delete as required

• Panel: 	80/20 vision Electrofused steel S235JR made up from triple flanged 50 x 1.5mm flat bar at 46mm centres vertically and 4mm wire at 132mm centres horizontally. Top and Bottom constructed from 50 x 3mm flat bar. Galvanised and polyester powder-coated to a minimum of 60 microns. * delete as required

100/0 vision Electrofused steel S235JR made up from triple flanged 69 x 1.5mm flat bar at 46mm centres vertically and 4mm wire at 132mm centres horizontally. Top and Bottom constructed from 50 x 3mm flat bar. Galvanised and polyester powder-coated to a minimum of 60 microns. * delete as required

• Posts: 	RHS or SHS depending upon application

• Fixings: 		Depending on application

• Set posts: 	Set posts in holes 300 mm diameter x 800** mm deep, filled not less than half the depth with concrete, as clause 620.

• Maximum post centers: 	1642mm/2032mm * delete as required (panel width 1992mm)

• Bottom of fencing to be: 	Maximum of 100 mm above final ground level.

• Other requirements: 	PPC Colour Green RAL 6005. A full range of RAL Colours are available including marine grade and metallics.

** Depending on fence height

NOTES: 	All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.