Specification clauses

To be read with Preliminaries/General conditions

Open mesh steel panel perimeter security fencing/gates

CLD Ultimate Extra Profiled Panel System.

• Height:		1800mm/2030mm/2430mm/3030mm* delete as required

• Nominal height: 	1.8m/2.0m/2.4m/3.0* delete as required

• Mesh & wire: 	165 x 25mm mesh; 6 mm nominal wire with 3 or 4* (delete as required) profiles, galvanised and polyester powder-coated to 60 microns.

- 3 Profiles 1800mm ONLY

- 4 Profiles 2030mm – 3030mm ONLY

• Posts: 	80 x 40 mm RHS, galvanised after manufacture and polyester powder-coated with 41 x 21mm clamping channel galvanised and polyester powder-coated to match fencing.

• Fixings: 		CLD ‘SafeTFix’ Hidden Fixing System

• Set posts: 	Set posts in holes 300 mm diameter x 800** mm deep, filled not less than half the depth with concrete, as clause 620.

• Maximum post centers: 	2485mm (1800 – 2430mm ONLY)* delete as required

2060mm (3030mm ONLY)* delete as required

• Bottom of fencing to be: 	approx. 50 mm above final ground level.

• Other requirements: 	PPC Colour Green RAL 6005. A full range of RAL Colours are available from CLD Fencing Systems including marine grade and metallics.

** Depending on fence height

NOTES: 	All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.