Specification clauses

To be read with Preliminaries/General conditions

Open steel panel perimeter security fencing/gates

CLD Securogril Rigid Panel System.

• Height:	930mm/1194mm/1326mm/1458mm/1722mm/1986mm/2118mm/2514mm (fencing can be made up of a combination of the above panels) * delete as required

• Nominal height: 	1.0m/1.2m/1.4m/1.5m/1.8m/2.0m/2.2m/2.6m (fencing can be made up of a combination of the above panels) * delete as required

• Panel: 	Electrofused steel S235JR made up from 25 x 2mm flat bar at 62mm centres vertically and 4.5mm wire at 132mm centres horizontally. Top and Bottom constructed from 25 x 4mm flat bar. Galvanised and polyester powder-coated to a minimum of 60 microns.

• Posts: 	RHS or SHS depending upon application

• Fixings: 		Depending on application

• Set posts: 	Set posts in holes 300 mm diameter x 800** mm deep, filled not less than half the depth with concrete, as clause 620.

• Maximum post centers: 	2032mm

• Bottom of fencing to be: 	Maximum of 100 mm above final ground level.

• Other requirements: 	PPC Colour Green RAL 6005. A full range of RAL Colours are available including marine grade and metallics.

** Depending on fence height

NOTES: 	All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.