Specification clauses

To be read with Preliminaries/General conditions

Open mesh steel panel sports fencing/gates

CLD Sports Rail Mesh Panel System with Top Rail

• Height:	990mm/1190mm/1390mm * delete as required

• Nominal height: 	1.0m/1.2m/1.4m * delete as required (other heights available on request)

• Mesh & wire: 	Dulok Rebound Double Wire Rigid Mesh Panel 50 x 66.5mm rebound mesh; 6mm verticals and twin 8mm horizontal nominal wires, galvanised and polyester powder-coated to 60 microns. * delete as required

Dulok Sports 868 Double Wire Rigid Mesh Panel 200 x 50mm mesh; 6mm verticals and twin 8mm horizontal nominal wires, galvanised and polyester powder-coated to 60 microns. * delete as required

Dulok Sports 656 Double Wire Rigid Mesh Panel 200 x 50mm mesh; 5mm verticals and twin 6mm horizontal nominal wires, galvanised and polyester powder-coated to 60 microns. * delete as required

Securus 358 Rigid Mesh Panel 76.2 x 12.5 mm mesh; 4 mm wire, high aluminium content galvanised and polyester powder-coated to minimum 80 microns * delete as required

Exempla Profiled Rigid Mesh Panel 200 x 50mm mesh; 5mm wires with 2 profiles, galvanised and polyester powder-coated to 60 microns. * delete as required

• Posts: 	60 x 40 mm RHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

48.3 mm CHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

60.3 mm CHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

• Top Rail:	60 x 40 mm RHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

48.3 mm CHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

60.3 mm CHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

• Fixings: 	CLD Sports Rail clamps and fixings as supplied by manufacturer

• Set posts: 	Set posts in holes 300 mm diameter x 800** mm deep, filled not less than half the depth with concrete, as clause 620.

• Maximum post centers: 	2495mm (Exempla ONLY) / 2520mm * delete as required

• Bottom of fencing to be: 	approx. 50 mm above final ground level.

• Other requirements: 	PPC Colour Green RAL 6005. A full range of RAL Colours are available including marine grade and metallics.

** Depending on fence height

NOTES: 	All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.