Specification clauses

To be read with Preliminaries/General conditions

Open mesh steel panel sports fencing/gates

CLD Velodrome Safety Handrail System with Single/Twin Top Rail

• Height:	930mm

• Nominal height: 	1.1m

• Mesh & wire: 	Securus 358 Rigid Mesh Panel 76.2 x 12.5 mm mesh; 4 mm wire, high aluminium content galvanised and polyester powder-coated to minimum 80 microns

• Posts: 	48.3 mm CHS with cross rails to support mesh, galvanised after manufacture and polyester powder-coated to match fencing.

• Top Rail:	42 mm CHS, galvanised after manufacture and polyester powder-coated to match fencing. * delete as required

• Fixings: 	M8 security bolt with 100 x 5mm full length clamp bar, galvanised and polyester powder-coated after manufacture to match fencing.

• Set posts: 	Set posts in holes 350 mm diameter x 600 mm deep, filled full depth with concrete, as clause 620.

• Maximum post centers: 	1.5m as per manufacturers details

• Bottom of fencing to be: 	approx. 30 mm above final ground level.

• Other requirements: 	PPC Colour Green RAL 6005. A full range of RAL Colours are available from CLD Fencing Systems including marine grade and metallics.

NOTES: 	To be read in STRICT conjunction with manufacturers drawings.

All dimensions are nominal, for further information please contact Farm Relief Fencing. All information is correct at time of production. We reserve the right to alter specification without notice.